CITY OF DETROIT

SPECIFICATIONS

FOR

CONCRETE PAVEMENT REPAIR

DET: GJM								                       11-25-2015

Description.  This work shall be in accordance with Section 603. Concrete Pavement Restoration, of the MDOT 2012 Standard Specifications for Construction, and MDOT Standard Plan R-44-F for Concrete Pavement Repair.  The work shall consist of saw cutting as necessary for removal of existing concrete base with HMA overlay, preparation of sub base, placing horizontal dowels, placing concrete, joints, finishing, and curing.

Construction.  HMA Leveling Course placed over the concrete base repair area shall be removed and paid for in accordance with MDOT Sections 204 and 501 as HMA Surface, Rem.

When removing existing concrete pavement, the pavement shall be removed to an existing joint, or saw cut to a true line with a vertical face along the lines as marked or directed by the Engineer.  The pavement shall be saw cut full depth into existing concrete, or as directed by the Engineer.  Intermediate saw cuts shall be made as required by Section 603, referenced above.  The removal shall be such that there will be no disturbance and/or damage to sections of pavement which are to remain in place.  All damaged or undermined pavement caused by the Contractors operations shall be removed and replaced at the Contractor's expense.  The use of a crane and ball type breaking equipment will not be allowed.  Pavement removal shall be accomplished with a rubber-tired hydraulic ram or as specified in Section 603 of the MDOT Standard Specifications.

Where subgrade corrections are required due to undesirable or unstable soil conditions as determined by the Engineer, the removal of material and placement of fill shall be performed in accordance with MDOT Section 205, and paid for as Subgrade Undercutting, Type II.

All replacement concrete pavement shall be doweled or anchored to the existing concrete pavement as set forth on Standard Plan R-44-F.  All expansion and longitudinal joints shall be restored.  Transverse joints within partial width cuts shall be restored to match the joint in other lanes.  Transverse joints that fall within full width cuts need not be restored.

The top of the concrete pavement repair shall be placed level with the HMA Leveling Course.

Measurement and Payment.  All material, labor and equipment required for constructing concrete pavement repair as specified herein and as shown on the Standard Plans shall be paid for under the unit rates bid for as follows:

Pavt Repr, Rem, Modified, shall include all labor, equipment and material to perform the concrete base pavement removal work, including all saw cutting.

Pavt Repr, Nonreinf Conc, __ inch, Modified, shall include all labor, material and equipment to place the concrete pavement repair including all dowels, anchors, joints, concrete material, finishing and curing.

Pay Item								Pay Unit

Pavt Repr, Rem, Modified						Square Yard

Pavt Repr, Nonreinf Conc, 8 inch, Modified				Square Yard

Pavt Repr, Nonreinf Conc, 10 inch, Modified				Square Yard

HMA Surface, Rem							Square Yard

Subgrade Undercutting, Type II					Cubic Yard