CITY OF DETROIT

SPECIFICATION

FOR

HMA APPLICATION

DET: GJM		              				            	                 10-05-15

Description:  This Specification covers the furnishing and placing of Hot Mixed Asphalt in accordance with Section 501 of the 2012 MDOT Standard Specifications for Construction.

Material:  HMA materials shall be as specified in Section 501.02.

The HMA Leveling Surfacing Mixture 4E3 shall have a yield of 220 pounds per square yard with an estimated thickness of 2 inches.

The HMA Top Surfacing Mixture 5E3 shall have a yield of 165 pounds per square yard with an estimated thickness of 1.5 inches.

Performance Grade; PG 64-22

The material for HMA Approach shall be 2 inches of HMA Mixture 4E3 for leveling, and 1.5 inches of HMA Mixture 5E3 for top surface, having a total yield of 385 pounds per square yard.

The material for Hand Patching shall be 3 inches minimum of HMA Mixture 5E3, having a yield of 330 pounds per square yard (or as directed by the Engineer).

HMA Shoulder, Modified (Driveway Approach) shall be HMA Mixture 5E3, having a yield of 165 pounds per square yard.

HMA Prime Coat and HMA Bond Coat shall be included in the HMA pay item and shall meet the requirements specified in Section 904 of the 2012 MDOT Standard Specifications for construction.

The aggregate wear index shall be 260.

Construction:  The HMA shall be produced and placed in accordance with Section 501.03 of the 2012 MDOT Standard Specifications for Construction.

Measurement and Payment:  The unit price bid shall be full compensation for all labor, equipment, and materials required to place the HMA as specified.

Pay Item										Pay Unit

HMA, 4E3										Ton

HMA, 5E3										Ton

HMA Approach									Ton

HMA Shoulder, Modified								Ton